## Slide 1: Material Analysis: Thermal Gap Filler
Jean Kim, Advanced Polymeric Materials Branch Intern
Witold Fuchs, Ph.D Advanced Polymeric Materials Branch, M&P Technical Lead
Notes: “Thermal Decomposition analysis of AEPS soft goods”

## Slide 2: Bottom-line up front (BLUF)
Objective: Identify the material composition of Thermal Gap Filler
Instruments: FTIR, TGA, Outgassing
Conclusion: The binder material is most likely polyester

## Slide 3
Chart: Transmittance vs Wavenumber (cm-1)
Fourier Transform Infrared spectroscopy (FTIR) Results
Comparing to known spectra of polymer: The associated peak at around ~1750 cm-1at ester position, indicates C=O bond (Carbonyl)
Shamsun Nahar, Sultana & Rahaman, Md Samsur & Samadder, Rajib & Rahaman, Faisal S & Chadni, R. & Khan, Mubarak. (2022). A Modified Hydrolysis Method of Decolorizing Reactive-Dyed Polycotton Waste Fabric and Extraction of Terephthalic Acid: A Perspective to Reduce Textile Solid Waste.
Asymmetrical C-H Stretching (CH3)
At around ~2920 cm-1
Symmetrical C-H Stretching (CH2)
At around ~2850 cm-1
Notes: FTIR Functional Group Database Table with Search – InstaNANO

## Slide 4
Thermogravimetric Analysis (TGA) Results
Chart: Weight(%) vs Time(min) TGA Ramp 10.00 °C/min to 125.00 °C, Isothermal for 12 hrs
Ferreira, Marcos Vinícius & Neves, Anna & Oliveira, Caroline & Perissé Duarte Lopes, Felipe & Margem, Frederico & Vieira, Carlos Maurício & Monteiro, Sergio. (2017). Thermogravimetric characterization of polyester matrix composites reinforced with eucalyptus fibers.
The TGA result shows similar trend to neat polyester
Notes: FTIR Functional Group Database Table with Search – InstaNANO

## Slide 5: Summary
FTIR results show that the material is organic with C-H and C=O bonding. By comparing the positions of distinct peaks against known spectra, the material contains polyester-based filler.
TGA results further confirms the typical behavior of polyester.
The material is most likely contains polyester-based filler