## Slide 1: Material Characterization: Polyimides Alternative
Jean Kim, Advanced Polymeric Materials Branch Intern
Witold Fuchs, Ph.D Advanced Polymeric Materials Branch, M&P Technical Lead
Notes: “Thermal Decomposition analysis of AEPS soft goods”

## Slide 2
Polymer | Max Temp | Injection Mold | Relative Cost | Outgas Performance (TML%)
PEI | ~170C | YES | $/2 | Refer to August 4th Roxy(Alyssa)’s presentation for the up-to-date outgassing performance values
PPS | ~200C-220C | YES | $$ | 
PEEK | ~250C | YES | $$ | 
TPI | ~260C | YES | $$ | 
PEKK | ~260C-300C | YES | $$$ | 
Thermoset PI | ~315-340C | No (Composite/Press) | $$$$$$$$$$ (10) | 
Machined PI | ~300C (Short 480C) | No (Machined only) | $$$$$$$$$$$$$$$$$$ (18) | 
PBI | ~315C-400C (Short 500C) | No (Machined only) | $$$$$$$$$$$$$ (13) | 
*Acceptable TML% as per ASTM-E595 standard is 1.00%
Each $ sign is roughly $500.
Notes: PEI: Polyetherimide
PPS: Polyphenylene Sulfide
PEEK: Polyetheretherketone
TPI: Thermoplastic Polyimide
- Short term high temperature resistance is quite high.
PEKK: Polyetherketoneketone
- Highest Temp tolerance that can be injection molded.
Thermoset PI: Thermoset Polyimides
Machined PI: Machined Polyimides
PBI: Polybenzimidazole - Highest-performing engineering plastic in existence.

## Slide 3
Material | Price per Piece | Notes
PEI | $289.36 | 
PPS | $1,003.05 | 
PEEK | $722.00-772.26 | 
TPI | N/A | Domestic vendor not available
PEKK | $1,000-$2,000+ | Domestic vendor not available Price may vary
Thermoset PI | $3,000~$7,000+ | Domestic vendor not available Price may vary
Machined PI | $6,000~$12,000 | Domestic vendor not available Price may vary
PBI | $4,500+ | Domestic vendor not available Price may vary
Sheet 12 in × 12 in × 0.5

## Slide 4
Material | Price per Piece | Notes
PEI | N/A | Domestic vendor not available
PPS | $570.00/kg | Price may vary.
PEEK | $1380.00/kg | 
TPI | N/A | Domestic vendor not available (Request quote for exact pricing))
PEKK | $1650.00/kg | Price may vary.
Thermoset PI | X | Not injection moldable.
Machined PI | X | Not injection moldable.
PBI | X | Not injection moldable.
Granules/Pellets (Injection Molding)